1/4” CORK SPECIFICATIONS

| Property | Test Method | Result | Unit |
| --- | --- | --- | --- |
| Specific Gravity: | ASTM D3676 | 0.19 min |  |
| Tensile Strength: | ASTM F152 | 65 | PSI |
| Compression: Recovery: | ASTM F36 | 22 max 75 min | 100 PSI percent |
| Boiling Fluid Immersion Test: | ASTM F 148 | Boiling Water Boiling HCL | Pass Pass |
| Mildew Resistance Test: |  | Pass | Factor |
| Thermal Conductivity: | "K" Factor "R" Factor | .40 2.6 | btu/sf/h/F/inch 1/4" |
| Acoustical properties under and hardwood / laminate floors |
|  | Absorbs 84% of reflected sound Absorbs 69% of transmitted sound |
| Acoustical properties under hardwood floors |
|  | Impact Nose Rating (INR) Impact Insulation Class (ICC) Sound Transmission Class (STC) | +7 56 54 |
|  | Meets and/or exceeds Specification: |
|  |  | HH-C-576 Type II MIL C-15116C Type II |

| Physical Properties |
| --- |
| Cork Underlay: |
| Width: | 36" (3 ft) | standard |
| Density | 200-220kgs/sqm. 6mm (1/4") | Standard |
| Thickness: | 6mm (1/4") | Standard |