Specifications for Sound Solution EVA

- Provides superior sound absorption and the most realistic hardwood walk sounds available

- Made from PET, 100% recycled materials

- The Green Choice in flooring underlayment

- Advanced water proof technology

- Save energy, save money with year round protection against heat & cold loss through your floor

- Water proof & vapor proof protective thermal layer

- Resilient – maintains original structure

- 3 in 1 – includes overlap

- Antimicrobial mold and mildew inhibitor

- EVA Foam with Aluminum Film

- Class (IIC) = 71

- ASTM – E492-90 (ASTM-E989-89)

- Sound Transmission Loss

- Class (STC) = 73

- ASTM-E90-02 (ASTM-E413-87)

- “R” Value – 3.19 (ft2 – f – hr/Btu-in)

- Thickness  3mm  (standard )